PIEZOELECTRIC CERAMIC, POLYMER and ceramic/polymer composite DEVICES - TYPES, MATERIALS, APLLICATIONS, NEW DEVELOPMENTS, INDUSTRY structure AND GLOBAL MARKETS

Traditional applications of piezoelectric devices are ultrasonic medical imaging, ultrasonic non-destructive testing, ultrasonic sensors, vehicle knock sensors, acoustic devices such as speakers, beepers, ceramic resonators, ultrasonic welding, ultrasonic cleaning, vibration cancellation, and sonars for military and civil use. Some new and growing applications include actuators, ultrasonic motors, sensor arrays for structural health monitoring, oil and gas field sensors, transformers and micro energy harvesting devices which are an alternative to batteries in microwatt devices. Other new applications include high resolution ultrasonic medical imaging, computer disk drives, and accelerometers in mobile phones and notebooks.

The piezoelectric device sector is actually not a single sector, but rather comprises a number of sectors with distinctly different characteristics. The sectors of most significance are:

- the piezoelectric device sector, with high production volume, consisting of generic piezoelectric devices such as actuators, motors, sensors, accelerators, transducers for ultrasonic medical imaging and non-destructive testing acoustic devices, Lengevin actuators for ultrasonic welding and cleaning, ceramic resonators, and miscellaneous types of devices designed for special applications such as transformers, vibration and noise cancellation in structures limited to different grades of piezoelectric crystals, ceramics such as PZT, PVDF and composites;

- sonars for military and civil use; and.

- niche applications such as energy harvesting, where piezoelectric devices such as generators offer a unique competitive advantage.

Piezo devices also include ultrasonic motors (USMs), which offer a high potential for miniaturization. These actuators produce no magnetic field since the excitation is quasi-electrostatic. Through their specific advantages compared to conventional electromagnetic motors, USMs fill a gap in certain actuator applications. A key advantage of USMs over electromagnetic motors is their compactness, i.e. their high stall torque-mass ratio and high torque at low rotational speed, often making speed-reducing gears superfluous. Additionally, with no voltage applied, an inherent holding torque is present due to the frictional driving mechanism. It is also worthwhile to mention that their compactness and the high frequency electrical excitation make quick responses possible.

study goal and objectives

This study focuses on key piezoelectric devices and provides data about the size and growth of the piezoelectric devices markets, company profiles and industry trends. The goal of this report is to provide a detailed and comprehensive multi-client study of the markets in North America, Europe, Japan, China, Korea and the rest of the world (ROW) for piezoelectric ceramic, polymer and ceramic/polymer composite devices, as well as potential business opportunities in the future.

A primary objective of this report is thorough coverage of underlying economic issues driving the piezoelectric ceramic and polymer devices business, as well as assessments of new, advanced piezoelectric devices that are being developed. Another important objective is to provide realistic market data and forecasts for piezoelectric devices. This study provides the most thorough and up-to-date assessment that can be found anywhere on the subject. The study also provides extensive quantification of the many important facets of market development in piezoelectric devices throughout the world. This, in turn, contributes to a determination of the kinds of strategic responses companies may adopt in order to compete in these dynamic markets.

Users of piezoelectric devices in developed markets must contend with twin pressures – to innovate and, at the same time, to reduce costs. New applications for piezoelectric devices have been proposed in recent years. This study condenses all of these business-related issues and opportunities.

REASONS FOR DOING THE STUDY

The piezoelectric devices market is a diversified but attractive and still-growing multi-billion dollar market characterized by very high production volumes of a diversified range of piezoelectric devices that must be both extremely reliable and low in cost. Growth in the piezoelectric devices market continues to be driven by increasing demands in camera phones for autofocus mechanisms, piezo transformers, energy harvesting devices, data storage, semiconductors, microelectronics production, precision mechanics, life science and medical technology, optics, photonics, nanometrology, robots, toys, HVAC control systems, hand-held consumer electronic devices, automotive sensors, ultrasonic transducers for medical imaging and non-destructive testing and vibration related applications, structural health monitoring, ultrasonic welding and cleaning, ceramic resonators for mobile phones and devices used for information and communication technologies. Since sonars for military and civil uses and other applications constitute an established market, we have included this segment in this report.

The diversified piezoelectric ceramic device business is complex and fast moving, with manufacturers increasingly adopting a truly global view of the market. Around the world, consumers are demanding high power density as well as extremely long cycle life. In this challenging market, manufacturers have attempted to achieve growth through company mergers and acquisitions and by implementing global strategies. Traditional piezoelectric devices have a broad customer base, and new applications such as ceramic resonators in mobile phones, transformers in notebooks, and energy harvesting are new areas that have now entered the mainstream and are showing significant sales volumes.

The global market for traditional piezoelectric devices is quite mature in applications. However, the global market for new piezoelectric devices will see even a much higher growth rate in next five years.

With this background of new emerging technologies, applications and markets, iRAP felt a need to conduct a detailed study and update technology developments and markets. The report identifies and evaluates piezoelectric ceramic, polymer and ceramic/polymer composite devices and technologies which show potential growth.

Contributions of the study

This study provides the most complete accounting of the current market and future growth in piezoelectric devices in North America, Europe, Japan, China and the rest of the world. It provides the most thorough and up-to-date assessment that can be found anywhere on the subject. The study also provides extensive quantification of the many important facets of market developments in emerging markets, such as China, for piezoelectric devices. This quantification, in turn, contributes to the determination of what kind of strategic response suppliers may adopt in order to compete in these dynamic markets. Audiences for this study include directors of technology, marketing executives, business unit managers and other decision makers in the piezoelectric devices companies, as well as in companies peripheral to this business.

SCOPE AND FORMAT

The market data contained in this report quantify opportunities for piezoelectric ceramic and polymer materials and devices. In addition to product types, this report also covers the merits and future prospects of the piezoelectric ceramic and polymer devices business, including corporate strategies, information technologies, and the means for providing these highly advanced product and service offerings. This report also covers in detail the economic and technological issues regarded by many as critical to the industry’s current state of change. It provides a review of the piezoelectric ceramic devices industry and its structure, and of the many companies involved in providing these products. The competitive positions of the main players in the piezoelectric devices market and the strategic options they face are also discussed, along with such competitive factors as marketing, distribution and operations.

TARGET AUDIENCE FOR THE STUDY

The study will benefit existing manufacturers of piezoelectric actuators, ultrasonic motors, sensors, transducers, transformers, resonators and micro- energy harvesting devices that seek to expand revenues and market opportunities by expanding and diversifying in vast applications of devices based on piezo materials like PZT, PVDF and composites of PZT and PVDF, which are positioned to become a preferred solution for many applications. Also, this study will benefit users of piezoelectric-operated actuators and motors where electromagnetic field generation is an issue and operational performance parameters and space are important considerations, such as in autofocus lens mechanisms of camera phones, nanometrology, precision linear/rotary drives, drug delivery systems, antenna array deployment, and other fields.

REPORT SUMMARY

The global market for traditional piezoelectric devices is quite mature in applications. However, the global market for new piezoelectric devices will see a much higher growth rate in next five years.

New applications are emerging for piezoelectric devices, which include applications based on actuators, ultrasonic motors, sensor arrays for structural health monitoring, transformers and micro-energy harvesting devices which are an alternative to batteries in microwatt devices. Other new applications include high resolution ultrasonic medical imaging, computer disk drives, and accelerometers in mobile phones and notebooks.

Unlike other piezo devices, commercialization of piezoelectric-operated actuators and motors is likely to proceed in those markets where the specific advantages of high torque, high precision and lack of magnetic interference are particularly useful. When the costs can be lowered to competitive levels, and remaining technical problems such as frictional wear can be solved, piezoelectric motors may also become candidates in areas such as automotive accessories, where very high volume markets are possible.

Major findings of this report are:

- The global market for the existing eleven generic types of piezoelectric ceramic, polymer and ceramic/polymer devices was estimated to have reached U.S. $20.6 billion in 2012 and is expected to reach $38.4 billion by 2017.

- Among the 2012 applications, the largest share goes to equipment for semiconductor manufacturing and testing, lab equipment, sensors and accelerators. The next biggest segment is piezo devices used in mobile phones, digital cameras, laptops and other consumer electronic equipment, where piezo devices used include six categories of devices – ultrasonic motors, piezo transformers, resonators, acoustic devices, sensors (primarily SAW sensors), and piezo generators.  This is followed by medical transducers, mini-grippers, dentist tools, ultrasonic non-destructive testing, vibration testing, welding and cleaning, telecommunication, traffic control, piezo print heads, gas ignitions and diesel injectors. Sonar for military and civil use constitutes the final segment..

- Among the eleven product-type market segments in 2012, actuators have the largest share of the market, followed by ultrasonic motors, sonar, piezo sensors and accelerators, acoustic devices, and smaller shares for Langevin actuators, piezo transformers, resonators and other miscellaneous types.

- New devices such as piezoelectric generators will see the highest growth rate from 2012 to 2017.  This category is followed by ceramic resonators, and miscellaneous applications (acousto-optic modulators in telecommunication engineering, vibrators, diesel/gasoline injectors and dentistry surgery tools).

- Traditional devices also will see growth, including acoustic devices, actuators, Langevin actuators for welding and cleaning, sonars, transducers, gas igniters and piezo printing heads.

- In 2012, Japan has the highest market share, followed by Europe, China, North America, Korea, and the rest of the world. By 2017, China is projected to occupy the top position ahead of Japan.

PIEZOELECTRIC CERAMIC, POLYMER and ceramic/polymer composite DEVICES - TYPES, MATERIALS, APLLICATIONS, NEW DEVELOPMENTS, INDUSTRY structure AND GLOBAL MARKETS

TABLE OF CONTENTS

TABLE OF CONTENTS

INTRODUCTION	1

STUDY GOAL AND OBJECTIVES	2

REASONS FOR DOING THE STUDY	3

CONTRIBUTIONS OF THE STUDY	4

SCOPE AND FORMAT	4

METHODOLOGY	4

INFORMATION SOURCES	5

TARGET AUDIENCE FOR THE STUDY	5

AUTHOR’S CREDENTIALS	6

RELATED STUDIES	6

EXECUTIVE SUMMARY	8

SUMMARY TABLE  GLOBAL MARKET SIZE/PERCENTAGE SHARES FOR PIEZOELECTRIC- OPERATED DEVICES BY PRODUCT TYPE,

2012 AND 2017	10

SUMMARY FIGURE	11

GLOBAL MARKET SHARE FOR PIEZOELECTRIC-OPERATED DEVICES BY TYPE, 2012 AND 2017	11

INDUSTRY STRUCTURE AND MARKET DYNAMICS	13

INDUSTRY STRUCTURE AND MARKET DYNAMICS (CONTINUED)	14

INDUSTRY STRUCTURE AND MARKET DYNAMICS (CONTINUED)	15

INDUSTRY STRUCTURE AND MARKET DYNAMICS (CONTINUED)	16

TECHNOLOGY OVERVIEW	17

THE PIEZOELECTRIC EFFECT	17

FERROELECTRIC DOMAINS AND POLARIZATION TO

PIEZOELECTRIC	17

DIRECT AND INVERSE PIEZO EFFECTS	18

ORTHOGONAL SYSTEM FOR PIEZOELECTRIC MATERIALS	18

FIGURE 1  ORTHOGONAL SYSTEM TO DESCRIBE PIEZOELECTRIC MATERIALS	19

MODES OF PIEZOELECTRIC EFFECTS	19

TABLE 1  FIVE MODES OF PIEZOELECTRIC EFFECTS	20

DEFINITIONS OF COMMON TERMINOLOGIES USED IN PIEZOELECTRIC MATERIAL AND DEVICES	21

PIEZOELECTRIC CHARGE CONSTANT	21

PIEZOELECTRIC VOLTAGE CONSTANT	21

PERMITTIVITY	22

ELECTROMECHANICAL COUPLING FACTOR	23

DIELECTRIC DISSIPATION FACTOR (DIELECTRIC LOSS FACTOR)	24

CURIE TEMPERATURE	24

MECHANICAL QUALITY FACTOR	24

TABLE 2  DEFINITIONS USED TO EXPRESS CHARACTERISTICS  OF PIEZOELECTRIC DEVICES	25

REQUIRED FUNCTIONAL CHARACTERISTICS OF DEVICES	26

PIEZO CHARACTERISTICS OF PZT MATERIALS	27

TABLE 3 COMPARISON OF HARD AND SOFT PZT PROPERTIES	27

PIEZOELECTRIC CERAMICS AND APPLICATIONS	28

Lead titanate	29

Lead metaniobate	29

Lead magnesium niobate – lead titanate (pmn-pt)	29

Bismuth titanate	29

CLASSES OF ACTIVE CERAMICS (PZT)	29

PZT MANUFACTURING PROCESS	30

PZT APPLICATIONS	31

PZT APPLICATIONS (CONTINUED)	32

ALTERNATIVE PIEZOELECTRIC MATERIALS	33

PVDF	33

PVDF (CONTINUED)	35

PVDF (CONTINUED)	35

PIEZOELECTRIC COPOLYMERS	36

PIEZOELECTRIC COMPOSITES	37

FIGURE 2  THREE PHASES OF PVDF MATERIAL	38

TABLE 4   INDIVIDUAL PROPERTIES OF PZT AND PVDF	39

TABLE 5  PROPERTIES OF PIEZOELECTRIC COMPOSITE AT DIFFERENT POLING FIELDS	39

TYPES OF CERAMIC-POLYMER COMPOSITES	41

MANUFACTURING PROCESS	42

PROPERTIES	43

TABLE 6  PIEZOELECTRIC PROPERTIES OF SOME TRANSDUCTION MATERIALS	43

PROPERTIES (CONTINUED)	44

APPLICATION SEGMENTS	45

ACTUATORS	45

ACTUATORS (CONTINUED)	46

BIMORPH ACTUATORS	47

Construction	47

Characteristics	48

Usage	49

UNIMORPH ACTUATORS	49

BUILDING-BLOCK ACTUATORS	50

FREQUENCY-LEVERAGED ACTUATORS	51

MULTILAYER ACTUATORS	51

Construction	52

OTHER ACTUATOR APPLICATIONS	53

X-Y STAGE FOR MICROSCOPE APPLICATIONS AND DIGITAL SLIDE IMAGING SYSTEMS	53

CERAMIC SERVO MOTORS	55

CERAMIC SERVO MOTORS (CONTINUED)	55

CERAMIC SERVO MOTORS (CONTINUED)	56

CERAMIC SERVO MOTORS (CONTINUED)	57

HIGH VOLUME APPLICATIONS	58

PRECISION MECHANICS	59

DATA STORAGE	60

ROBOTS AND TOYS	60

HVAC BUILDING CONTROL SYSTEMS	61

INTERIOR LIGHTING	61

BIOMEDICAL APPLICATIONS	62

ULTRASONIC MOTORS	63

SQUIGGLE MOTORS FOR CAMERA PHONES	63

TECHNOLOGY OF PIEZOELECTRIC-OPERATED MOTORS	65

TABLE 7  PIEZOELECTRIC MOTOR (TRAVELING WAVE) TYPICAL COMMERCIAL SIZES	66

TECHNOLOGY OPIEZOELECTRIC OPERATED MOTORS

(CONTINUED)	67

TABLE 8  KEY PIEZOELECTRIC MOTOR CHARACTERISTICS	68

LANGEVIN ACTUATORS	68

FIGURE 3  SCHEMATIC DIAGRAM OF A LANGEVIN-TYPE ACTUATOR	69

ULTRASONIC CLEANING	70

PIEZO TRANSFORMERS	70

FIGURE 4  TYPICAL PIEZO TRANSFORMER	71

TRANSONERS	72

CERAMIC RESONATORS	73

SURFACE ACOUSTIC WAVE (SAW) RESONATORS USING CERAMICS	74

TABLE 9  PREFERRED MATERIALS FOR SURFACE ACOUSTIC WAVE DEVICES	74

FIGURE 5  CONSTRUCTION OF CERAMIC SURFACE ACOUSTIC WAVE RESONATORS	75

FILM BULK ACOUSTIC RESONATORS (FBARS)	75

FIGURE 6  CONSTRUCTION OF CERAMIC SURFACE THIN FILM BULK ACOUSTIC WAVE RESONATOR	76

Bulk acoustic wave (baw) resonators	76

FIGURE 7  CONSTRUCTION OF BULK ACOUSTIC WAVE RESONATOR	77

TABLE 10 COMPARISON OF CERAMIC RESONATORS	77

TRANSDUCERS	78

NOISE REDUCTION/VIBRATION DAMPING APPLICATIONS	79

TABLE 11  CHARACTERSTICS OF PIEZOELECTRIC ULTRASONIC TESTING PROBES	80

Examples of vibration reduction	80

FIGURE 8  ACTIVE VERSUS PASSIVE VIBRATION DAMPING	81

Vibration measurement (accelerometers)	83

Nondestructive testing	84

Market for nondestructive testing equipment	85

Ultrasonic testing equipment manufacturing	86

PIEZO GENERATORS	87

SINGLE-LAYER PIEZOELECTRIC GENERATORS	87

FIGURE 9  SINGLE-LAYER PIEZOELECTRIC GENERATORS	88

MULTILAYER PIEZOELECTRIC GENERATORS	88

ENERGY HARVESTING/BATTERY ALTERNATIVES	89

FIGURE 10  SCHEMATIC REPRESENTATION OF THE PIEZOELECTRIC ENERGY HARVESTING PROCESS	90

FIGURE 11  COMPARISON OF THE ENERGY DENSITY FOR THE THREE TYPES OF MECHANICAL TO ELECTRICAL ENERGY CONVERTERS	91

PIEZO GENERATORS (CONTINUED)	92

SONARS FOR MILITARY AND CIVILIAN USE	93

FIGURE 12  CLASSIFICATION OF SOUND BY FREQUENCY LEVEL	94

ACTIVE SONAR	94

PASSIVE SONAR	96

TABLE 12 PIEZOELECTRIC CERAMIC VOLUME

FRACTION SELECTED IN PZT/PVDF COMPOSITE DEVICES FOR SONARS	97

TABLE 13  REQUIRED CHARACTERSTICS OF PIEZOELECTRIC SONAR/HYDROPHONE ELEMENTS FOR NAVY	97

PIEZOELECTRIC SENSORS	99

TABLE 14  PIEZOELECTRIC ACCELERATORS AND SENSORS IN SPECIAL APPLICATIONS	99

ULTRASONIC FLOW METERS	101

ULTRASONIC SENSORS	102

HUMIDITY SENSORS	102

PRESSURE SENSORS	102

POSITION SENSORS	103

KNOCK SENSORS	104

ULTRASONIC LEVEL SENSORS	104

TABLE 15  COMPARISION OF CHARACTERSTICS OF PIEZO SENSORS BY DIFFERENT TECHNOLOGIES	105

TABLE 16  CHARACTERSTICS OF PIEZOELECTRIC SENSORS	106

ACCELEROMETERS	106

ACOUSTIC DEVICES	108

CAR ALARMS	109

BEEPERS	109

SIRENS	109

SPEAKERS	110

MICROPHONES	110

RECEIVERS	110

HEADPHONES	111

TABLE 17  REQUIRED CHARACTERSTICS OF ACOUSTIC DEVICES	111

MISCELLANEOUS APPLICATIONS	111

HIGH-VOLTAGE DEVICES/GAS IGNITORS	112

PIEZO PRINT HEADS	113

DIESEL INJECTORS	113

LASER MIRROR ALIGNMENT	114

ACOUSTO-OPTIC MODULATORS	114

PIEZOELECTRIC DRIVERS AND AMPLIFIERS	114

ULTRASONIC VIBRATORS	115

PIEZO CABLE FOR TRAFFIC CONTROL	115

ULTRASONIC DENTAL SCALERS	116

PIEZOELECTRIC DEVICES IN VEHICLES	116

TABLE 18 TYPICAL AUTOMOTIVE PIEZO APPLICATIONS	117

FIGURE 13 ILLUSTRATION OF TYPICAL AUTOMOTIVE PIEZO APPLICATIONS	118

PIEZOELECTRIC DEVICES IN SAFETY AND SECURITY PRODUCTS	118

TABLE 19 SAFETY AND SECURITY APPLICATIONS FOR PIEZO DEVICES

RF APPLICATIONS	121

FIGURE 14 ILLUSTRATION OF WIRELESS SENSOR NETWORKS	123

CONSUMER ELECTRONICS AND PIEZOELECTRIC DEVICES	124

TABLE 20 APPLICATION OF PIEZO DEVICES IN CONSUMER ELECTRONICS	127

FIGURE 15  ILLUSTRATION OF GLOBAL TECH MARKET GROWTH	128

NONDESTRUCTIVE TESTING AND PIEZOELECTRIC DEVICES	128

TABLE 21 APPLICATIONS OF PIEZO DEVICES IN NONDESTRUCTIVE TESTING	129

MARKETS	133

TABLE 22  GLOBAL MARKET SIZE/PERCENTAGE SHARE FOR PIEZOELECTRIC OPERATED DEVICES BY PRODUCT TYPE,

2012 AND 2017	134

FIGURE 16   MARKET SHARE FOR PIEZOELECTRIC DEVICES BY TYPE, 2012 AND 2017	135

PIEZOELECTRIC ACTUATORS	136

TABLE 23  GLOBAL MARKET DISTRIBUTION OF PIEZOELECTRIC ACTUATORS BY APPLICATION, 2012 AND 2017	137

ACTUATORS (CONTINUED)	138

FEATURES OF PIEZOELECTRIC ACTUATORS	139

TABLE 24 PIEZO APPLICATIONS IN MOTORS, ACTUATORS AND SENSORS	141

ACTUATORS (CONTINUED)	141

SEMICONDUCTOR TECHNOLOGY	143

BIOTECHNOLOGY AND LIFE SCIENCES	143

MEDICAL DESIGN	144

MICROSCOPY	146

DATA STORAGE TECHNOLOGY	146

NANOTECHNOLOGY AND AUTOMATION	147

AERONAUTICS, IMAGE PROCESSING	147

ASTRONOMY, ADAPTIVE OPTICS	148

METROLOGY, LASER SYSTEMS	148

PRECISION MACHINING AND DIAMOND TURNING	148

PHOTONICS, TELECOM AND INTEGRATED OPTICS	149

ULTRASONIC MOTORS	149

ULTRASONIC MOTORS (CONTINUED	150

ULTRASONIC MOTORS (CONTINUED	152

TABLE 25  MARKET SHARE ACCORDING TO APPLICATIONS FOR PIEZOELECTRIC-DRIVEN ULTRASONIC MOTORS/CERAMIC SERVO MOTORS, 2012 AND 2017	153

LANGEVIN ACTUATORS	155

TABLE 26  GLOBAL MARKET DISTRIBUTION OF LANGEVIN ACTUATORS BY APPLICATION, 2007, 2012 AND 2017	156

PIEZOELECTRIC ACTUATORS AND MOTORS MARKET	156

TABLE 27 GLOBAL MARKET SIZE/PERCENTAGE SHARE FOR PIEZOELECTRIC ACTUATORS AND MOTORS BY APPLICATION, THROUGH 2018	157

PIEZO TRANSFORMERS	158

TABLE 28 MARKET FOR PIEZO TRANSFORMERS, 2012-2017	158

RESONATORS	160

TABLE 29 MARKET FOR PIEZO RESONATORS, 2012-2017	160

PIEZO GENERATORS/ENERGY HARVESTING	162

TABLE 30 COMPANIES AND PRODUCTS USING PIEZOELECTRIC ENERGY HARVESTERS DEVELOPED BY ENOCEAN	163

TABLE 31 COMPANIES AND ORGANIZATIONS DEVELOPING ENERGY HARVESTING PIEZOELECTRIC DEVICES	166

TABLE 32 MAKRKET FOR PIEZO GENERATORS, 2012-2017	171

TRANSDUCERS	171

TABLE 33 GLOBAL MARKET DISTRIBUTION OF PIEZOELECTRIC TRANSDUCERS BY APPLICATION, 2007, 2012 AND 2017	172

SONARS FOR MILITARY AND CIVILIAN USE	173

TABLE 34 GLOBAL MARKET FOR SONARS FOR MILITARY AND CIVILIAN USE, 2007, 2012 AND 2017	175

PIEZO SENSORS AND ACCELERATORS	176

TABLE 35 GLOBAL MARKET DISTRIBUTION OF PIEZOELECTRIC SENSORS BY APPLICATION, 2007, 2012 AND 2017	177

ACOUSTIC DEVICES	178

TABLE 36  GLOBAL  MARKET FOR PIEZOELECTRIC ACOUSTIC DEVICES THROUGH 2017	179

ADDITIONAL PIEZOELECTRIC DEVICES	179

TABLE 37  GLOBAL MARKET FOR MISCELLANEOUS PIEZOELECTRIC-OPERATED DEVICES, 2007, 2012 AND 2017	180

MARKET SEGMENTS BY APPLICATION	181

TABLE 38 USAGE OF PIEZOELECTRIC DEVICES BY APPLICATION	181

TABLE 39 GLOBAL MARKET SIZE AND PERCENTAGE SHARE FOR PIEZOELECTRIC-OPERATED DEVICES BY APPLICATION,	183

2007, 2012 AND 2017	183

MARKET SEGMENTATION BY PIEZOELECTRIC MATERIALS	184

TABLE 40  GLOBAL MARKET FOR PIEZOELECTRIC-OPERATED DEVICES	185

SEGMENTED BY MATERIAL USED, 2012-2017	185

FIGURE 17 MARKET SHARE ACCORDING TO TYPE OF PIEZOELECTRIC MATERIAL USED IN DEVICES, 2012 AND 2017	186

MARKET SEGMENTATION BY REGION	186

TABLE 41 SUMMARY OF MARKET OF PIEZOELECTRIC DEVICES BY REGION THROUGH 2017	187

FIGURE 18  REGIONAL PERCENTAGES OF MARKET SHARE FOR PIEZOELECTRIC DEVICES, 2012 AND 2017	188

MARKET SEGMENTATION BY REGION (CONTINUED)	189

INDUSTRY STRUCTURE AND DYNAMICS	191

MARKET STRUCTURE (CONTINUED)	191

TABLE 42 PIEZOELECTRIC MATERIAL SUPPLIERS PRODUCT LINE REFERENCE	192

MARKET STRUCTURE (CONTINUED)	193

MARKET STRUCTURE (CONTINUED)	194

MARKET SHARE OF COMPANIES	195

COMPETITION	197

MERGERS, ACQUISITIONS AND DIVESTITURES	198

TABLE 43 ACQUISITIONS AND JOINT VENTURES AMONG MANUFACTURERS OF PIEZOELECTRIC DEVICES FROM 2004 TO 2012

BUSINESS MODELS AND PLAYERS	200

TABLE 44  PIEZOELECTRIC DEVICE SUPPLIERS PRODUCT LINE REFERENCE	201

NEW DEVELOPMENTS	205

NEW MATERIALS AND PRODUCTS	205

PIEZOELECTRIC KINETIC ENERGY HARVESTER FROM NOKIA	206

PIEZOELECTRIC COOLER FROM GE	206

TEMPERATURE-COMPENSATED PIEZOELECTRIC SUBSTRATES FROM ZIPTRONIX	207

PIEZOELECTRIC NANOFIBERS	208

NEW PROCESSES	209

NEW APPLICATIONS	210

NEW DEVICES	210

PIEZOELECTRIC TRANSFORMERS	211

PIEZOELECTRIC CERAMIC COUPLER	211

MEDICAL	212

Chem-lab-on-a-chip	212

Antibody-based piezoelectric nanobiosensors	212

Piezoelectrically-based smart micro- and nanostructures and systems	213

FUTURE RESEARCH AND DEVELOPMENT TRENDS	213

FUTURE R&D TRENDS (CONTINUED)	214

PATENTS AND PATENT ANALYSIS	216

LIST OF PATENTS	216

PIEZOELECTRIC DEVICES	216

MULTI-LAYER PIEZOELECTRIC ELEMENT, AND INJECTION APPARATUS AND FUEL INJECTION SYSTEM THAT EMPLOY

THE SAME	216

STACKED PIEZOELECTRIC DEVICE	217

APPARATUS FOR GENERATING ELECTRICAL ENERGY USING ELECTRICALLY CONNECTED NANOWIRE AND ACTIVE LAYER AND METHOD FOR MANUFACTURING THE SAME	217

INJECTION MOLDED ENERGY HARVESTING DEVICE	218

ACOUSTIC POWER GENERATOR AND METHOD FOR MANUFACTURING THE SAME	218

DOWNHOLE PIEZOELECTRIC DEVICES	218

MICRO-SPEAKER AND MANUFACTURING METHOD THEREOF	219

ULTRASONIC PROBE, ULTRASONIC DIAGNOSTIC APPARATUS AND ULTRASONIC ENDOSCOPIC APPARATUS	219

METHOD FOR DRIVING LIQUID EJECTOR	219

ENERGY HARVESTING POWER SOURCES FOR ASSISTING IN THE RECOVERY/DETONATION OF UNEXPLODED MUNITIONS	220

SYSTEM FOR CONVERTING OCEAN WAVE ENERGY TO ELECTRIC POWER	220

LIQUID DROPLET JETTING APPARATUS AND LIQUID DROPLET JETTING HEAD	221

ENERGY HARVESTING POWER SOURCES FOR GENERATING A TIME-OUT SIGNAL FOR UNEXPLODED MUNITIONS	221

ACOUSTIC RESONATOR PERFORMANCE ENHANCEMENT USING SELECTIVE METAL ETCH	222

TUBULAR LINEAR PIEZOELECTRIC MOTOR	222

ELASTIC WAVE DEVICE AND ELECTRONIC COMPONENT	222

BISTABLE PIEZOELECTRIC GENERATOR	223

METHOD OF MANUFACTURING PIEZOELECTRIC ACTUATOR AND METHOD OF MANUFACTURING LIQUID TRANSPORTING

APPARATUS	223

DIFFERENTIATION AND IDENTIFICATION OF ANALOGOUS CHEMICAL AND BIOLOGICAL SUBSTANCES WITH BIOSENSORS	224

PIEZO-EFFECT TRANSISTOR DEVICE AND APPLICATIONS	224

HIGH POWER ULTRASOUND TRANSDUCER	225

METHOD OF MANUFACTURING A PIEZOELECTRIC ACTUATOR	225

ORTHOPEDIC APPLIANCE	225

METHOD AND AEVICE FOR CONTROLLING THE ROTATION SPEED OF A PIEZOELECTRIC MOTOR ROTOR	226

METHOD OF MANUFACTURING A PIEZOELECTRIC TRANSISTOR	226

MULTILAYER PIEZOELECTRIC ACTUATOR AND LIQUID DISCHARGE HEAD	226

INTEGRATED ACOUSTIC BANDGAP DEVICES FOR ENERGY CONFINEMENT AND METHODS OF FABRICATING SAME	227

TIRE MODULE WITH PIEZOELECTRIC TRANSDUCER	227

ANTI-EMI ULTRASONIC TRANSDUCER	228

PIEZOELECTRIC ACTUATORS	228

PIEZOELECTRIC-BASED NANOPORE DEVICE FOR THE ACTIVE CONTROL OF THE MOTION OF POLYMERS THROUGH THE SAME	229

TIRE MODULE WITH PIEZOELECTRIC CONVERTER	229

RESONANT ACTUATOR	229

STICK-SLIP PIEZOELECTRIC MOTOR	230

METHOD OF MANUFACTURING ORIENTATION FILM AND METHOD OF MANUFACTURING LIQUID DISCHARGE HEAD	230

PIEZOELECTRIC PHASE SHIFTER	231

PIEZOELECTRIC ACTUATION STRUCTURE INCLUDING AN INTEGRATED PIEZORESISTIVE STRAIN GAUGE AND ITS

PRODUCTION METHOD	231

MULTILAYERED PIEZOELECTRIC ELEMENT AND METHOD OF PRODUCING THE SAME	231

ULTRASONIC MECHANICAL EMULSIFIER	232

PIEZOELECTRIC PRESSURE CONTROL VALVE	232

ULTRASONIC TRANSDUCER AND ULTRASONIC APPARATUS HAVING THE SAME	233

CURVED TWO-DIMENSIONAL ARRAY TRANSDUCER	233

TOUCH AND AUDITORY SENSORS BGASED ON NANOTUBE ARRAYS	234

ELECTRICALLY CONTROLLABLE LATCH MECHANISM	234

PANEL-TYPED LOUD SPEAKER AND AN EXCITER THEREFOR	234

PIEZOELECTRIC ACTUATOR AND ELECTRONIC DEVICE	235

PIEZOELECTRIC ACTUATOR AND METHOD FOR MANUFACTURING PIEZOELECTRIC ACTUATOR	235

ACOUSTIC TRANSDUCER SYSTEM FOR NONDESTRUCTIVE TESTING OF CEMENT	236

METHOD OF DRIVING PIEZOELECTRIC INK JET HEAD	236

PIEZOELECTRIC RESONATOR ELEMENT, PIEZOELECTRIC DEVICE AND GYRO SENSOR	237

IDT ELECTRODED PIEZOELECTRIC DIAPHRAGMS	237

PIEZOELECTRIC SCAN SYSTEM	237

PIEZOCABLE BASED SENSOR FOR MEASURING UNSTEADY PRESSURES INSIDE A PIPE	238

SYSTEM AND METHOD OF MEASURING QUASI-STATIC FORCE WITH A PIEZOELECTRIC SENSOR	238

NOISE REJECTING ELECTRONIC STETHOSCOPE	239

ROTOR POSITION SENSING APPARATUS AND METHOD USING PIEZOELECTRIC SENSOR AND HALL-EFFECT SENSOR	239

DISK DRIVE LOAD ARM STRUCTURE HAVING A STRAIN SENSOR AND METHOD OF ITS FABRICATION	239

LIGHT TRIGGERED LIGHT SWITCH	240

PIEZOELECTRIC FILTER, ANTENNA DUPLEXER, AND COMMUNICATIONS APPARATUS EMPLOYING PIEZOELECTRIC RESONATOR	240

MICROMACHINED IMAGING TRANSDUCER	240

METHOD OF DETECTING ACCELERATION IN VEHICLES	241

ACTIVE SENSOR FOR MICRO FORCE MEASUREMENT	241

PIEZOELECTRIC CERAMICS	242

METHODS OF FABRICATING A MEMBRANE WITH IMPROVED MECHANICAL INTEGRITY	242

COMPOSITIONS FOR HIGH POWER PIEZOELECTRIC CERAMICS	242

PIEZOELECTRIC THIN FILM, INK JET HEAD, METHOD FOR FORMING IMAGE WITH THE INK JET HEAD, ANGULAR VELOCITY SENSOR, PIEZOELECTRIC GENERATING ELEMENT	243

LEAD-FREE PIEZOELECTRIC MATERIAL	243

SPUTTERED PIEZOELECTRIC MATERIAL	243

PIEZOELECTRIC MATERIAL AND PIEZOELECTRIC ELEMENT	244

PIEZOELECTRIC/ELECTROSTRICTIVE CERAMIC COMPOSITION CONTAINING 30-50 MOL% TA AND PIEZOELECTRIC/ELECTRORESTRICTIVE DEVICE CONTAINING

THE SAME	244

PIEZOELECTRIC MICROCANTILEVERS AND USES IN ATOMIC FORCE MICROSCOPY	245

PIEZOELECTRIC CERAMIC AND PIEZOELECTRIC ELEMENT	245

PIEZOELECTRIC CERAMIC, VIBRATOR AND ULTRASONIC MOTOR	245

SHEAR MODE-TYPE PIEZOELECTRIC ACTUATOR AND LIQUID DROPLET EJECTION HEAD	246

PIEZOCERAMIC DEVICE	246

HIGH-TEMPERATURE DIELECTRIC MATERIALS AND CAPACITORS MADE THEREFROM	246

MEMS PIEZOELECTRIC SWITCH	247

BOND PAD FOR USE WITH PIEZOELECTRIC CERAMIC SUBSTRATES	247

HIGH TEMPERATURE PIEZOELECTRIC MATERIAL	248

BIMORPH MIRROR WITH TWO PIEZOELECTRIC LAYERS SEPARATED BY A CENTRAL CORE OF SEMIRIGID MATERIAL	248

PIEZOELECTRIC DEVICE	248

PIEZOELECTRIC VIBRATOR	249

ACCELERATION SENSOR	249

ACOUSTIC STACK FOR ULTRASONIC TRANSDUCERS AND METHOD FOR MANUFACTURING SAME	250

PIEZOELECTRIC LINEAR MOTOR WITH DISPLACEMENT AMPLIFYING MEANS	250

RESONATOR	251

ZOOM LENS MODULE	251

METHOD FOR MANUFACTURING PIEZOELECTRIC ACTUATOR	251

PIEZOELECTRIC ULTRASONIC MOTOR FOR 2-DIMENSIONAL POSITIONING	252

PIEZOELECTRIC ACTUATOR, INSPECTION METHOD, AND LIQUID EJECT APPARATUS	252

COMPOSITIONS FOR HIGH POWER PIEZOELECTRIC CERAMICS	253

MULTILAYER PIEZOELECTRIC ELEMENT, FUEL INJECTOR HAVING THE PIEZOELECTRIC ELEMENT AND PIEZOELECTRIC ELEMENT PRODUCTION METHOD	253

METHOD FOR THE PRODUCTION OF MONOLITHIC MULTILAYER ACTUATOR MADE OF A PIEZOCERAMIC OR ELECTROSTRICTIVE MATERIAL AND EXTERNAL ELECTRICAL CONTACT FOR THE SAME	254

MANUFACTURING METHOD FOR MONOLITHIC PIEZOELECTRIC

PART, AND MONOLITHIC PIEZOELECTRIC PART	254

HOLLOW LAMINATED PIEZOELECTRIC ELEMENT AND ITS MANUFACTURING METHOD	255

CAMERA AND PIEZO CERAMIC MOTOR THEREFOR	255

PROCESS FOR THE MANUFACTURE OF PIEZOCERAMIC MULTILAYER ACTUATORS	255

NON-SYMMETRIC DRIVE TYPE PIEZOELECTRIC CERAMIC TRANSFORMER	256

PIEZO ACTUATOR COMPRISING A STRUCTURED EXTERNAL ELECTRODE	256

PIEZOELECTRIC POLYMERS	257

HYBRID ELECTRIC DEVICE USING PIEZOELECTRIC POLYMER SUBSTRATE	257

PIEZOELECTRIC POLYMER SENSOR DEVICE	257

PIEZOELECTRIC COMPOSITE DEVICES	258

ELECTRET COMPOSITE WITH DEEP TRAPPING CENTERS ON THE INTERPHASE BOUNDARY	258

MICROMACHINED PIEZOELECTRIC ULTRASOUND TRANSDUCER ARRAYS	258

PIEZOELECTRIC COMPOSITE BEAM WITH AUTOMATICALLY ADJUSTABLE NATURAL FREQUENCY	258

MULTI-LAYER GAS MATRIX PIEZOELECTRIC COMPOSITE TRANSDUCER	259

METHOD FOR MAKING AN ACOUSTIC TRANSDUCER	259

METHOD OF PRODUCING A PIEZOCOMPOSITE	260

PATENT ANALYSIS	260

TABLE 45  NUMBER OF U.S. PATENTS GRANTED TO COMPANIES   MANUFACTURING PIEZOELECTRIC DEVICES FROM 2007 THROUGH OCTOBER 2012	261

INTERNATIONAL OVERVIEW OF U.S. PATENT ACTIVITY IN PIEZOELECTRIC-OPERATED DEVICES	263

TABLE 46  U.S. PATENTS GRANTED TO COUNTRIES/REGIONS FOR PIEZOELECTRIC DEVICES FROM JAN. 2007 TO 2012	264

OPERATED DEVICES (CONTINUED)	265

SYSTEM FOR CONVERTING OCEAN WAVE ENERGY TO ELECTRIC POWER	265

ANTI-EMI ULTRASONIC TRANSDUCER	265

CAMERA AND PIEZO CERAMIC MOTOR THEREFOR	266

BISTABLE PIEZOELECTRIC GENERATOR	266

LIGHT TRIGGERED LIGHT SWITCH	266

COMPANY PROFILES	267

AIRMAR TECHNOLOGY CORPORATION	267

AITO BV	268

ALPHA CERAMICS, INC.	268

--------------

--------------

--------------

Y. STERN ENGINEERING	318

ZIPTRONIX	319

ZONARE MEDICAL SYSTEMS	319

t.