PERMANENT MAGNETS – Types, applications, new developments, industry structure and global markets

Permanent magnets are a vital part of modern life. They are found in or used to produce almost every modern convenience today, from speakers in mobile phones to the electric motors in hybrid cars; air conditioners and washing machines. Permanent magnets are used increasingly in technological applications, including traveling wave tubes, Hall Effect sensors, high temperature-resistant permanent magnets, thin-film coating equipment and flywheel storage systems.

In all of these applications, it is important for the designed permanent magnet to be of high strength, resistive to corrosion, and resistive to demagnetization due to excessive heat. Manufacturers have gained experience in designing and producing permanent magnets to meet these needs for industries with permanent magnet and magnetic assembly applications.

There are a number of major families of permanent magnets available for designers, ranging from ferrite, known for its low cost and low energy, to rare earth materials, which are more expensive and offer higher performance. Designers need to analyze magnetizing field strength and magnetic output of magnetic materials prior to deciding on the appropriate magnet.

Permanent magnets today are 60 times as strong as they were about 90 years ago. Strong permanent magnets that can be used in industrial applications were developed in the 20th century, and Japanese and western European researchers and technologies have always played major roles in the development of permanent magnets.

With the heavy reliance on Neo magnets in manufacturing, rare earth (RE) materials neodymium and dysprosium are playing a very important role because of the scarcity of these materials and the dominance of a single country (China) in providing them. The permanent magnet industry will start to see the end of serious RE shortages as new supplies begin to hit the market during 2013 and beyond, with new designs and new materials.

study goals and objectives

This iRAP report has been prepared to highlight the many new developments in the permanent magnet industry. Many of the market segments are mature, while others are growing at very fast rates. Developing economies such as China and India are also emerging as growth engines for many industries that use permanent magnets. The markets in these new economies are expected to experience maximum revenue growth during the next five years.

Secondly, there are new applications for permanent magnets such as voice coil motors, traveling wave tubes, wind turbine generators, hybrid and pure electric vehicle motors, water turbine generators, thin-film coating equipment and flywheel storage systems applications. These have created the need for a formal analysis of technological and business issues, trends in manufacturing, competitive landscapes and Chinese domination in global markets, as well as factors such as shortages of raw materials used in Neo magnets.

This report has been prepared to:

- provide an overview of the various permanent magnets, their production technologies and applications;

- identify the technological and business issues related to the commercial production of permanent magnets;

- understand the inter-material competition among the various permanent magnets;

- determine the current size and future growth of the global markets for permanent magnets till 2018;

- identify and profile global producers, distributers, fabricators and suppliers of permanent magnets;

- assess new global funding in research of RE-free permanent magnet materials; and

- illustrate US patents in this field that were granted between 2009 and 2013.

REASONS FOR DOING THE STUDY

Piezoelectric devices, combined with the development of piezoelectric materials, have become a key enabling technology for a wide range of industrial and consumer products. The piezoelectric device market experienced robust growth in last two decades and sustained fairly healthy growth even during the global economic downturns. It will again witness strong growth in the next years, and certain application markets already enjoy double digital growth.

The industrial and manufacturing area is still the largest application market for piezoelectric devices, followed by the automotive industry. However, the strongest demand comes from medical instruments and information and telecommunication, which are gaining ever-increasing importance among piezoelectric device suppliers.

The piezoelectric actuator and motor market is an attractive and still-growing multi-million dollar market characterized by very high production volumes of actuators and motors that must be both extremely reliable and low in cost. Growth in the market continues to be driven by increasing demand in camera phones for autofocus mechanisms, data storage, semiconductors, micro-electronics production, precision mechanics, life science and medical technology, optics, photonics, nanometrology, robots, toys, HVAC control systems, and other applications such as piezo fuel injectors, ink cartridges in printers, micropumps, microgrippers. microsurgery tools and piezoelectric MEMS (piezo MEMS) actuators.

iRAP conducted this study in 2007 and later in 2009. However, with increased demand for these devices, and with improved and emerging technologies as well as applications, iRAP felt a need to conduct a detailed study and update technology developments and markets. The report identifies and evaluates piezoelectric-operated actuators and motors and technologies which show potential growth.

Contributions of the study

This technical/economic study covers technical and industry overviews, materials, current and emerging production methods, business and technology issues, current and emerging applications, industry structure and an extensive market analysis. Current size and future growth of the global markets are estimated for 2013 and 2018.

FORMAT AND SCOPE

This report reviews the technology of permanent magnet materials, types of permanent magnet materials and their applications, and current and anticipated demand for specific materials. For each material segment, the report provides an analysis of material and product types in that category, processing technologies, properties, applications, the global markets and foreign competition.

The qualitative and quantitative judgments embodied in this report are a valuable contribution to the current knowledge of permanent magnets, their manufacturing technologies, applications and markets. Moreover, this study has been conducted at a vital stage when new magnet materials such as neodymium-iron-boron are revolutionizing applications. Because of the miniaturization of electronic components and computers, more powerful and smaller magnets are needed for such applications. This current study identifies all such applications.

Company profiles of all global producers of permanent magnets are covered, along with major distributors, fabricators and a listing of leading consumers of permanent magnets.

TO WHOM THE STUDY CATERS

This report is directed to companies that are interested in the developments in this field such as:

- companies involved in the development, manufacturing and supplying of advanced materials;

- manufacturers and suppliers of permanent magnets;

- manufacturers and suppliers of systems and subsystems which incorporate permanent magnets;

- manufacturers and suppliers of raw materials for permanent magnets;

- importers and suppliers of permanent magnets;

- users of permanent magnets; and

- advanced materials companies interested in diversification.

REPORT SUMMARY

The permanent magnet industry has grown in the last decade and is likely to continue this growth into the next decade because of increased usage of magnetic circuit components in a variety of industrial equipment and devices. Electromechanical devices constitute the largest market for permanent magnet materials. This market is growing rapidly. Large motors use ceramic magnets, and, for certain military applications, samarium-cobalt (Sam-Co) is still the preferred magnet.

Applications related to permanent magnet direct current motors – brushless direct current (BLDC) and brush-type (PMDC) – and power generation will be the largest usage segment of neodymium-iron-boron (NdFeB) permanent magnets, followed by voice coil motors (VCMs) in disk drives, because of the need for reduced size and higher performance. The third major usage segment is hybrid and electric automotive drives. Several rare earth (RE) elements are essential ingredients in the highest performance magnets available in the world today; these magnets have enabled miniaturization and a significant increase in power density in hundreds of applications.

The market experienced a boom in 2011, due to increased demand for RE permanent magnets. But as demand increased, supply chain interruptions resulted in a scarcity of RE permanent magnets. This affected the market adversely, and it plunged in 2012. As the supply of REs became stable, the market became stable, and it is expected to further stabilize in the future.

The permanent magnet market has a large number of small manufacturers coupled with a few medium-sized manufacturers. The market is dominated by Chinese manufacturers. There is a scarcity of manufacturers for rare earth magnets, and they are geographically scattered.

Major findings of this report are:

- The global market for permanent magnets has reached US$11.3 billion in 2013, and is expected to grow to US$ 15 billion by 2018 with a CAGR of 5.7%

- Metallic magnets (combining neodymium-iron-boron, alnico, and samarium-cobalt magnets) dominate the market in 2013, followed by ceramic magnets (ferrites) magnets. A distant third is the bonded magnets.

- In terms of regional demand, the market is large in the Asia-Pacific region, and it is growing at a fast pace due to rising demand from end-user industries, especially in countries such as China and Japan.

- The market is growing slowly in Europe, but will continue to grow at a significant rate in the North America.

- The market is still in its infancy in Africa and Latin America, but these regions are experiencing high growth because of increased infrastructure spending and a low base effect. This market will experience an escalation in the demand of permanent magnets in the years to come.

- The five-year period of 2013 through 2018 will see more of the industry centered in China.

- The U.S. is a net importer of permanent magnets, for as much as 60% of its consumption. However, the U.S. still dominates in high performance magnets used in military and other strategic applications.

PERMANENT MAGNETS – Types, applications, new developments, industry structure and global markets

TABLE OF CONTENTS

INTRODUCTION	1

STUDY GOALS AND OBJECTIVES	1

CONTRIBUTIONS OF THE STUDY	2

FORMAT AND SCOPE	3

METHODOLOGY AND INFORMATION SOURCES	3

WHO SHOULD SUBSCRIBE	4

AUTHOR’S CREDENTIALS	4

EXECUTIVE SUMMARY	6

SUMMARY TABLE- GLOBAL MARKET FOR PERMANENT MAGNETS	7

SUMMARY FIGURE-GLOBAL MARKET FOR PERMANENT MAGNET SEGMENTS  IN 2013 AND 2018	8

INDUSTRY OVERVIEW	9

INDUSTRY STRUCTURE	10

MARKET OVERVIEW	11

CHINA MARKET	12

U.S. MARKET	13

EUROPE	14

JAPAN	14

OTHER COUNTRIES	15

TECHNOLOGY AND APPLICATIONS	16

PERMANENT MAGNETIC MATERIALS	17

TABLE 1 - NOMINAL COMPOSITIONS, CURIE TEMPERATURES, AND MAGNETIC ORIENTATIONS OF SELECTED PERMANENT MAGNET MATERIALS	18

SUMMARY OF PROPERTIES	19

TABLE 2-SUMMARY OF RANGE OF PROPERTIES OF PERMANENT MAGNET MATERIALS	20

TABLE 3-NOMINAL MAGNETIC PROPERTIES OF SELECTED PERMANENT MAGNET MATERIALS	21

TABLE 4-NOMINAL MECHANICAL AND PHYSICAL PROPERTIES OF SELECTED PERMANENT MAGNET MATERIALS	22

TABLE 5-TERMS/DEFINITIONS RELATED TO PERMANENT      MAGNETS	23

CERAMIC HARD FERRITE MAGNETS	31

MATERIAL TYPES	31

MANUFACTURING PROCESSES	32

PROPERTIES	33

PHYSICAL AND MECHANICAL PROPERTIES	33

ELECTRICAL AND MAGNETIC PROPERTIES	33

TABLE 6-MAGNETIC PROPERTIES OF CHINESE CERAMIC MAGNETS	34

TABLE 7-EQUIVALENT MAGNETIC PROPERTIES OF U.S. VS. CHINESE HARD FERRITE CERAMIC MAGNETS	34

APPLICATIONS OF HARD FERRITES	34

TABLE 8-APPLICATIONS OF HITACHI’S RADIALLY ORIENTED RING CERAMIC MAGNETS	37

PRICING OF FERRITE MAGNETS	37

TABLE 9-PRICING OF COMMERCIALLY AVAILABLE FERRITE PRODUCTS	37

INDUSTRY STRUCTURE	38

LIST OF MANUFACTURERS	38

MARKET SHARES OF COMPANIES	39

TABLE 10-MARKET SHARE OF TOP MANUFACTURERS OF FERRITE MAGNETS IN 2013	39

GLOBAL MARKET SIZE	40

TABLE 11-GLOBAL MARKET OF HARD FERRITE PERMANENT MAGNETS,2013-2018	40

NEODYMIUM-IRON-BORON (ND-FE-B) RARE EARTH MAGNETS	41

MANUFACTURING PROCESSES	41

FIGURE 1-NEODYMIUM-IRON-BORON MAGNET PRODUCTION CYCLE	43

PROPERTIES, COMPOSITIONS AND GRADES	43

TABLE 12-MMPA DESIGNATIONS FOR RARE EARTH IRON-BORON MAGNETS	44

TABLE 13-MAGNETIC CHARACTERISTICS OF TDK’S NEOREC NDFEB MAGNETS	45

APPLICATIONS	45

TABLE 14-GLOBAL MARKET SHARE BY WEIGHT FOR NEODYMIUM-IRON-BORON MAGNETS BY APPLICATION 2013	46

AUTOMOTIVE INDUSTRY	46

HDDS, CDS, DVDS	47

ELECTRIC BICYCLES	47

TRANSDUCERS AND LOUDSPEAKERS	47

MAGNETIC SEPARATION	48

MRIS	48

TORQUE-COUPLED DRIVES	48

SENSORS	48

HYSTERESIS CLUTHES	49

GENERATORS	49

ENERGY STORAGE SYSTEMS	49

WIND POWER GENERATORS	50

FIGURE 2 CONVENTIONAL AND DIRECT DRIVE WIND TURBINES	50

AIR CONDITIONING COMPRESSORS AND FANS	50

HYBRID AND ELECTRIC DRIVES	51

OTHER USES	51

PRICE PATTERN OF NEODYMIUM-IRON-BORON MAGNETS	52

TABLE 15-PRICE PATTERN OF COMMERCIALLY AVAILABLE NEODYMIUM-IRON-BORON PERMANENT MAGNETS PRODUCTS	52

ISSUES AND CHALLENGES IN USE OF LIGHT EARTH METALS AND  HEAVY EARTH METALS (USE OF DYSPROSIUM IN NEODYMIUM-IRON-BORON PERMANENT MAGNETS)	53

NED-FE-B PERMANENT MAGNET ISSUES – AN OVERVIEW	54

INDUSTRY STRUCTURE	57

LIST OF MANUFACTURERS	57

TABLE  16-GLOBAL MANUFACTURERS OF NDFEB MAGNETS	58

GLOBAL MARKET SIZE	58

TABLE 17-GLOBAL MARKET FOR NEO PERMANENT MAGNETS, 2013 AND 2018	59

MARKET SIZE BY APPLICATION FOR NEODYMIUM-IRON-BORON PERMANENT MAGNETS	60

TABLE 18-GLOBAL MARKET FOR NEODYMIUM-IRON-BORON  MAGNETS BY APPLICATION, 2013 AND 2018	60

RARE-EARTH COBALT MAGNETS	63

MATERIALS AND TYPES	63

TABLE 19-RARE EARTH MAGNET DESIGNATIONS	64

TABLE 20-NOMINAL COMPOSITION, CURIE TEMPERATURE AND MAGNETIC ORIENTATION OF COMMERCIAL RARE-EARTH COBALT MAGNETS	65

RARE-EARTH COBALT 5	65

RARE-EARTH 2 TRANSITION METAL 17 GROUP	66

MANUFACTURING PROCESSES	66

PROPERTIES	67

PHYSICAL AND MECHANICAL PROPERTIES	68

TABLE 21-NOMINAL PHYSICAL AND MECHANICAL PROPERTIES OF   RE MAGNETS	68

MAGNETIC PROPERTIES	68

TABLE 22-NOMINAL MAGNETIC PROPERTIES OF RARE EARTH/COBALT MAGNETS	69

TABLE 23-MAGNETIC PROPERTIES OF SOME COMMERCIALLY AVAILABLE	70

RARE EARTH COBALT MAGNETS	70

APPLICATIONS	70

PRICE PATTERN OF SAMARIUM-COBALT PERMANENT MAGNETS	71

INDUSTRY STRUCTURE	72

LIST OF MANUFACTURERS	72

TABLE 24-GLOBAL MANUFACTURERS OF SAMARIUM-COBALT MAGNETS	72

GLOBAL MARKET	73

TABLE 25-GLOBAL MARKET OF SAMARIUM-COBALT   PERMANENT MAGNETS	73

ALNICO PERMANENT MAGNETS	74

MATERIALS AND TYPES	75

TABLE 26-ALNICO MAGNET DESIGNATIONS	76

AVAILABLE SHAPES AND SIZES	77

PROPERTIES	77

CAST ALNICOS	78

TABLE 27-NOMINAL COMPOSITION, CURIE TEMPERATURE AND MAGNETIC ORIENTATION OF CAST ALNICOS	79

TABLE 28-MAGNETIC PROPERTIES OF CAST ALNICO MAGNETS	80

TABLE 29-NOMINAL PHYSICAL AND MECHANICAL PROPERTIES  OF CAST ALNICO MAGNETS	81

SINTERED ALNICOS	81

TABLE 30-NOMINAL COMPOSITION, CURIE TEMPERATURE AND MAGNETIC ORIENTATION OF SINTERED ALNICOS	82

TABLE 31-MAGNETIC PROPERTIES OF SINTERED ALNICO MAGNETS	82

TABLE 32-NOMINAL PHYSICAL AND MECHANICAL PROPERTIES OF SINTERED ALNICO MAGNETS	83

MANUFACTURING PROCESSES	83

CAST ALNICOS	84

SINTERED ALNICOS	84

HEAT TREATMENT	84

FINISHING	85

APPLICATIONS	85

PRICE PATTERN OF ALNICO PERMANENT MAGNETS	85

TABLE 33-PRICE PATTERN OF COMMERCIALLY AVAILABLE ALNICO PRODUCTS	86

INDUSTRY STRUCTURE	86

LIST OF MANUFACTURERS	86

TABLE 34-LEADING GLOBAL MANUFACTURERS OF ALNICO    MAGNETS	87

GLOBAL MARKET SIZE	87

TABLE 35-GLOBAL MARKETS OF ALNICO PERMANENT MAGNETS	88

BONDED AND FLEXIBLE PERMANENT MAGNETS	89

MATERIALS AND TYPES	90

BONDING MATERIALS	90

COMPOSITIONS AND GRADES OF BONDED MAGNETS	90

TABLE 36-POWDER SPECIFICATIONS OF BONDED FERRITE	91

MANUFACTURING PROCESSES	92

PRODUCING BONDED MAGNETS VIA EXTRUSION	92

FIGURE 3-BONDED MAGNET PRODUCTION VIA EXTRUSION     PROCESS	93

PRODUCING BONDED MAGNETS VIA INJECTION MOLDING	93

FIGURE 4-BONDED MAGNET PRODUCTION VIA INJECTION MOLDING PROCESS	94

PRODUCING BONDED MAGNETS VIA COMPRESSION	94

FIGURE 5-BONDED MAGNET PRODUCTION VIA COMPRESSION MOLDING PROCESS	95

CALENDERING AND PRODUCING FLEXIBLE SHEET	95

FIGURE 6-BONDED MAGNET PRODUCTION VIA CALENDERING PROCESS	96

APPLICATIONS	96

TABLE 37-APPLICATIONS FOR TYTEK INDUSTRIES’ MAGNETS	97

TABLE 38 APPLICATIONS FOR TDK’S COMPOSITE MAGNETS	97

PRICE PATTERN OF BONDED MAGNETS	98

TABLE 39-AVERAGE PRICES OF FERRITE, SMCO AND NDFEB BONDED MAGNETS	98

INDUSTRY STRUCTURE	98

MAJOR MANUFACTURERS	99

TABLE 40-LEADING MANUFACTURERS OF BONDED MAGNETS IN CHINA, EUROPE, JAPAN, THE U.S., AND THE REST OF THE WORLD	99

GLOBAL MARKET	100

TABLE 41-GLOBAL MARKET FOR PERMANENT BONDED MAGNETS	100

FIGURE 7-GLOBAL MARKET FOR PERMANENT BONDED MAGNETS	101

OTHER MAGNETS	102

ELONGATED SINGLE DOMAIN (ESD) MAGNETS	102

IRON-CHROMIUM-COBALT MAGNET ALLOYS	102

MANUFACTURING	102

PROPERTIES	103

TABLE 42-MAGNETIC PROPERTIES OF IRON-CHROMIUM-COBALT MAGNETS	103

TABLE 43-MAGNETIC PROPERTIES OF HITACHI IRON-CHROMIUM-COBALT MAGNETS	104

APPLICATIONS	104

MAGNET ALLOYS	104

REMALLOY	104

TABLE 44-PHYSICAL AND MECHANICAL PROPERTIES OF REMALLOY	105

CUNIFE	105

TABLE 45-PHYSICAL AND MECHANICAL PROPERTIES OF CUNIFE	106

CUNICO	106

TABLE 46-PHYSICAL AND MECHANICAL PROPERTIES OF CUNICO	107

VICALLOY	107

TABLE 47-PHYSICAL AND MECHANICAL PROPERTIES OF VICALLOY	107

TABLE 48-NOMINAL COMPOSITIONS, CURIE TEMPERATURES  AND MAGNETIC ORIENTATION OF MAGNET ALLOYS	108

TABLE 49-NOMINAL MAGNETIC PROPERTIES OF MAGNET ALLOYS	108

MAGNET STEELS	109

TABLE 50-NOMINAL COMPOSITIONS, CURIE TEMPERATURES  AND MAGNETIC ORIENTATION OF MAGNET STEELS	109

FABRICATION	109

PHYSICAL AND MECHANICAL PROPERTIES	110

MAGNETIC PROPERTIES	110

TABLE 51-NOMINAL MAGNETIC PROPERTIES OF MAGNET STEELS	110

APPLICATIONS	111

PLATINUM COBALT	111

PHYSICAL AND MECHANICAL PROPERTIES	111

TABLE 52-NOMINAL MECHANICAL PROPERTIES OF                                 PT-CO MAGNETS	112

MAGNETIC PROPERTIES	112

TABLE 53-MAGNETIC PROPERTIES OF PT-CO MAGNETS	112

APPLICATIONS	113

MISCELLANEOUS PERMANENT MAGNET MATERIALS	113

TABLE 54-MAGNETIC PROPERTIES OF MISCELLANEOUS   PERMANENT MAGNET MATERIALS	113

NEW MAGNETIC MATERIALS UNDER DEVELOPMENT	114

TABLE 55-RARE EARTH FREE NEW MAGNETIC MATERIAL RESEARCH	115

INDUSTRY STRUCTURE	118

GLOBAL MANUFACTURERS	118

ADDITIONAL MARKET PARTICIPANTS	120

DISTRIBUTORS AND FABRICATORS	120

TABLE 56-GLOBAL DISTRIBUTORS AND FABRICATORS OF HARD FERRITE, ALNICO AND BONDED MAGNETS	121

TABLE 57-GLOBAL DISTRIBUTORS AND FABRICATORS OF NDFEB MAGNETS	122

TABLE 58-GLOBAL DISTRIBUTORS AND FABRICATORS OF SM-CO MAGNETS	123

COMPETITION AND MARKET TRENDS	123

TABLE 59-ACQUISITIONS, MERGERS, EXPANSIONS AND NEW RESEARCH FUNDING IN COMPANIES MANUFACTURING PERMANENT MAGNETS, 2009 TO JANUARY 2013	124

END USERS OF PERMANENT MAGNETS	128

TABLE 60-APPLICATIONS AND MAJOR END USERS OF PERMANENT MAGNETS IN THE U.S., EUROPE AND JAPAN	128

TABLE 61-CONTACT DETAILS FOR SOME SELECT END USERS OF PERMANENT MAGNETS IN THE U.S., EUROPE AND ASIA	129

MARKET SIZE AND SHARE	131

TABLE 62-GLOBAL MARKETS FOR PERMANENT MAGNETS	132

FIGURE 8-GLOBAL MARKET SHARE BY TYPE OF PERMANENT MAGNET	133

MARKET SIZE BY REGION	133

TABLE 63-GLOBAL OUTPUT OF PERMANENT MAGNETS BY REGION IN 2013	134

TABLE 64-GLOBAL OUTPUT OF PERMANENT MAGNETS BY REGION IN 2018	135

FIGURE 9-MAGNET PRODUCTION BY REGION	136

PATENTS AND PATENT ANALYSIS	137

PATENTS RELATED TO FERRITE PERMANENT MAGNETS	137

NON-AGEING PERMANENT MAGNET FROM AN ALLOY POWDER AND METHOD FOR THE PRODUCTION THEREOF	137

METHOD OF MANUFACTURING ROTOR MAGNET FOR MICRO ROTARY ELECTRIC MACHINE	137

HIGH SPEED INTERNAL PERMANENT MAGNET MACHINE AND METHOD OF MANUFACTURING THE SAME	138

FERRITE MATERIAL AND METHOD FOR PRODUCING FERRITE MATERIAL	138

SOFT MAGNETIC RIBBON, MAGNETIC CORE, MAGNETIC PART AND PROCESS FOR PRODUCING SOFT MAGNETIC RIBBON	139

MAGNET USING BINDING AGENT AND METHOD OF    MANUFACTURING THE SAME	139

FERRITE MATERIAL	140

PERMANENT MAGNET FOR MOTOR, MOTOR HOUSING, AND MOTOR DEVICE	140

PERMANENT MAGNET ROTATOR AND MOTOR USING THE SAME	140

METHOD FOR PREPARING RADIALLY ANISOTROPIC MAGNET	141

MAGNETIC ALLOY MATERIAL AND METHOD OF MAKING THE MAGNETIC ALLOY MATERIAL	141

PERMANENT MAGNET FOR PARTICLE BEAM ACCELERATOR AND MAGNETIC FIELD GENERATOR	142

PATENTS RELATED TO NEODYMIUM-IRON-BORON PERMANENT MAGNETS	142

R-FE-B RARE-EARTH SINTERED MAGNET AND PROCESS FOR PRODUCING THE SAME	142

RARE EARTH MAGNET AND METHOD FOR PRODUCING SAME	143

R-FE-B POROUS MAGNET AND METHOD FOR PRODUCING  THE SAME	143

METHOD FOR PREPARING RARE EARTH PERMANENT MAGNET MATERIAL	143

METHOD FOR PREPARING RARE EARTH PERMANENT MAGNET MATERIAL	144

RARE EARTH ALLOY BINDERLESS MAGNET AND METHOD FOR	144

MANUFACTURE THEREOF	144

RARE EARTH ELEMENT-IRON-BORON ALLOY, AND MAGNETICALLY ANISOTROPIC PERMANENT MAGNET POWDER AND METHOD FOR	145

PRODUCTION THEREOF	145

METHOD FOR PREPARING RARE EARTH PERMANENT MAGNET	145

RARE EARTH MAGNET AND METHOD FOR PRODUCTION THEREOF	145

IRON-BASED RARE-EARTH NANOCOMPOSITE MAGNET AND METHOD FOR PRODUCING THE MAGNET	146

METHOD FOR PRODUCING RARE EARTH METAL-BASED PERMANENT MAGNET HAVING COPPER PLATING FILM ON THE SURFACE THEREOF	147

RARE EARTH MAGNET AND METHOD FOR PRODUCING SAME	147

PROCESS FOR PRODUCING, THROUGH STRIP CASTING, RAW ALLOY FOR NANOCOMPOSITE TYPE PERMANENT MAGNET	148

METHOD FOR PRODUCING NANOCOMPOSITE MAGNET USING ATOMIZING METHOD	148

FUNCTIONALLY GRADED RARE EARTH PERMANENT MAGNET	149

FUNCTIONALLY GRADED RARE EARTH PERMANENT MAGNET	149

RARE EARTH PERMANENT MAGNET	150

PATENTS   RELATED TO BONDED AND FLEXIBLE PERMANENT MAGNETS	150

RARE EARTH BONDED MAGNET	150

R-FE-B RARE EARTH SINTERED MAGNET AND METHOD FOR PRODUCING SAME	151

R-FE-B TYPE RARE EARTH SINTERED MAGNET AND PROCESS FOR PRODUCTION OF THE SAME	151

RARE EARTH SINTERED MAGNET AND METHOD FOR PRODUCING SAME	151

R-T-B-TYPE SINTERED MAGNET AND METHOD FOR PRODUCTION THEREOF	152

ALLOY FOR SINTERED R-T-B-M MAGNET AND METHOD FOR PRODUCING SAME	152

FERRITE POWDERS FOR BONDED MAGNET, PROCESS FOR THE PRODUCTION OF THE POWDERS, AND BONDED MAGNET MADE BY USING THE SAME	153

ANISOTROPIC RARE EARTH-IRON BASED RESIN BONDED MAGNET	153

ROTATING MACHINE, BONDED MAGNET, MAGNET ROLL, AND METHOD FOR PRODUCING SINTERED FERRITE MAGNET	154

FERRITE MAGNET POWDER, SINTERED MAGNET, BOND MAGNET,  AND MAGNETIC RECORDING MEDIUM	154

PROCESS FOR PRODUCING SELF-ASSEMBLED RARE EARTH-IRON BONDED MAGNET AND MOTOR UTILIZING THE SAME	154

SINTERED R-FE-B PERMANENT MAGNET AND ITS PRODUCTION METHOD	155

YOKE-INTEGRATED BONDED MAGNET AND MAGNET ROTATOR FOR MOTOR USING THE SAME	155

ANISOTROPIC RARE EARTH BONDED MAGNET HAVING SELF-ORGANIZED NETWORK BOUNDARY PHASE AND PERMANENT  MAGNET MOTOR UTILIZING THE SAME	156

OXIDE MAGNETIC MATERIAL AND SINTERED MAGNET	156

OXIDE-TYPE, MAGNETIC MATERIAL AND ITS PRODUCTION         METHOD, AND SINTERED FERRITE MAGNET AND ITS PRODUCTION METHOD	157

R-T-B BASED SINTERED MAGNET	157

SINTERED R-FE-B PERMANENT MAGNET AND ITS PRODUCTION METHOD	157

YOKE-INTEGRATED BONDED MAGNET AND MAGNET ROTATOR FOR MOTOR USING THE SAME	158

ANISOTROPIC RARE EARTH BONDED MAGNET HAVING SELF-ORGANIZED NETWORK BOUNDARY PHASE AND PERMANENT   MAGNET MOTOR UTILIZING THE SAME	158

BOND MAGNET FOR DIRECT CURRENT REACTOR AND DIRECT CURRENT REACTOR	159

ANISOTROPIC BONDED MAGNET FOR USE IN A 4-POLE MOTOR, A MOTOR EMPLOYING THAT MAGNET, AND AN ALIGNMENT PROCESS APPARATUS FOR THE ANISOTROPIC BONDED MAGNET FOR USE IN A 4-POLE MOTOR	159

FERRITE MAGNETIC MATERIAL AND FERRITE SINTERED MAGNET	160

METHODS FOR PRODUCING RAW MATERIAL ALLOY FOR RARE  EARTH MAGNET, POWDER AND SINTERED MAGNET	160

METHODS FOR PRODUCING RAW MATERIAL ALLOY FOR RARE  EARTH MAGNET, POWDER AND SINTERED MAGNET	161

ANISOTROPIC BOND MAGNET FOR FOUR-MAGNETIC-POLE MOTOR, MOTOR USING THE SAME, DEVICE FOR ORIENTATION PROCESSING OF ANISOTROPIC BOND MAGNET FOR FOUR-MAGNETIC-POLE MOTOR 	161

ALLOY FLAKE FOR RARE EARTH MAGNET, PRODUCTION METHOD THEREOF, ALLOY POWDER FOR RARE EARTH SINTERED MAGNET, RARE EARTH SINTERED MAGNET, ALLOY POWDER FOR BONDED MAGNET AND BONDED MAGNET	162

METHOD FOR MANUFACTURING BONDED MAGNET AND METHOD  FOR MANUFACTURING MAGNETIC DEVICE HAVING BONDED  MAGNET	162

ISOTROPIC POWDERY MAGNET MATERIAL, PROCESS FOR PREPARING AND RESIN-BONDED MAGNET	163

PATENT ANALYSIS	163

TABLE 65-NUMBER OF U.S. PATENTS GRANTED TO COMPANIES IN THE PERMANENT MAGNET BUSINESS BY TYPE	164

FROM 2009 THROUGH APRIL 2013	164

TABLE 66-NUMBER OF U.S. PATENTS GRANTED TO COMPANIES IN THE PERMANENT MAGNET BUSINESS FROM 2009 THROUGH APRIL 2013	164

FIGURE 10-TOP COMPANIES GRANTED U.S. PATENTS FOR PERMANENT MAGNETS FROM 2009 THROUGH 2013	165

INTERNATIONAL OVERVIEW OF U.S. PATENT ACTIVITY IN PERMANENT MAGNETS	165

TABLE 67-U.S. PATENTS GRANTED FOR PERMANENT MAGNETS BY ASSIGNED COUNTRY/REGION FROM JANUARY 2009 TO APRIL 2013	166

COMPANY PROFILES	167

ADVANCED TECHNOLOGY & MATERIALS CO., LTD (AT&M)	167

ALLIANCE LLC	167

-----------------------------------------------------------

-----------------------------------------------------------

YUXIANG MAGNETIC MATERIALS INDUSTRIAL LIMITED	191

ZHEJIANG ANTE MAGNETIC MATERIAL CO., LTD.	191

DISTRIBUTORS AND FABRICATORS OF PERMANENT MAGNETS	192

ADAM MAGNETIC PRODUCTS CO.	192

ALLSTAR MAGNETICS	192

-----------------------------------------------------------

-----------------------------------------------------------

STANFORD MAGNETS	198

VIONA MAGNETICS	198

APPENDIX I: GLOSSARY OF TERMS	199

APPENDIX II: QUANTITIES, SYMBOLS, UNITS AND CONVERSION FACTORS	205